FINISHING SCHEDULE - INTERIOR

A. DRYWALL, WALLBOARD

Flat:

First Coat
1780 Proseal Vinyl Acrylic
Second Coat    
1776 Super Flat Vinyl Acrylic
or
1785 Pro Flat Wall Latex
1702  Flat Wall Latex

Satin:

First Coat          
1780 Proseal (Vinyl Acrylic)
or
1736 Excel Primer (100% Acrylic)
Second Coat      
1770 Super Satin (Vinyl Acrylic)
or
1805  Painters Satin Latex Enamel

Semi-Gloss:

First Coat            
1780 Proseal (Vinyl Acrylic)
or
1736 Excel Primer (100% Acrylic)
Second Coat      
1745 Super Semi-Gloss (100% Acrylic)
or
1750 Excel Semi-Gloss (100% Acrylic)

Gloss:

First Coat                  
1780 Proseal (Vinyl Acrylic)
or
1736 Excel Primer (100% Acrylic)
Second Coat            
1751 Excel Gloss (100% Acrylic)
or
Tech-Gard Gloss Enamel (Alkyd)
or
3017 Quick Dry Alkyd Gloss Enamel

B. PLASTER, CONCRETE, BLOCK

Flat:

First Coat                  
1738 Acrybond (Vinyl Acrylic- Aklyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat             
1776 Super Flat Vinyl Acrylic
or
1785 Pro Flat Wall Latex
1702  Flat Wall Latex

Satin:

First Coat            
1738 Acrybond (Vinyl Acrylic-Alkyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat      
1770 Super Satin (Vinyl Acrylic)
or
1805 Painters Satin Latex Enamel

Semi-Gloss:

First Coat          
1738 Acrybond (Vinyl Acrylic-Alkyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat      
1745  Super Semi-Gloss (100% Acrylic)
or
1750 Excel Semi-Gloss (100% Acrylic)

Gloss:

First Coat           
1738 Acrybond (Vinyl Acrylic-Alkyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat      
1751 Excel Gloss (100% Acrylic)
or
Tech-Gard Gloss Enamel (Alkyd)
or
3017 Quick Dry Alkyd Gloss Enamel

C. TILT-UP CONCRETE WALLS

Flat:

First Coat                  
1738 Acrybond (Vinyl Acrylic- Alkyd Modified
or
1736 Excel Primer (100% Acrylic)
Second Coat            
1776 Super Flat Vinyl Acrylic
or
1785 Pro Flat Wall Latex
1702  Flat Wall Latex

Satin:

First Coat                
1738 Acrybond (Vinyl Acrylic-Alkyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat            
1770 Super Satin (Vinyl Acrylic)
or
1805  Painters Satin Latex Enamel

Semi-Gloss:

First Coat             
1738 Acrybond (Vinyl Acrylic-Alkyd Modified)
or
1736 Excel Primer (100% Acrylic)
Second Coat          
1745 Super Semi-Gloss (100%  Acrylic)
or
1750 Excel Semi-Gloss (100% Acrylic)

C. CONCRETE TILT-UP WALLS (continued)

Gloss:

First Coat  
1738 Acrybond (Vinyl Acrylic-Alkyd Modified) or
1736 Excel Primer (100% Acrylic)
Second Coat 
1751 Excel Gloss (100% Acrylic)  or
Tech-Gard Gloss Enamel (Alkyd) or
3017 Quick Dry Alkyd Gloss Enamel

D. ACOUSTIC CEILINGS

Flat:

First Coat  
1785 Proflat (Vinyl Acrylic)
Second Coat  
1785 Profalt (Vinyl Acrylic)

E. SMOOTH WOOD-DOORS, CABINETS AND TRIM

Flat:

First Coat  
1758 Super Undercoat (100% Acrylic)
Second Coat  
1776 Super Flat (Vinyl Acrylic)

Satin:

First Coat  
1758 Super Undercoat (100% Acrylic)
Second Coat  
1770 Excel Satin (100% Acrylic)

Semi-Gloss:

First Coat  
1758 Super Undercoat (100% Acrylic)
Second Coat  
1750 Excel Semi-Gloss (100% Acrylic)

Gloss:

First Coat  
1758 Super Undercoat (100% Acrylic)
Second Coat  
1751 Excel Gloss (100% Acrylic) or
Tech-Gard Gloss Enamel (Alkyd) or
3017 Quick Dry Alkyd Gloss Enamel

F. SMOOTH WOOD- CLEAR LACQUER

Stain:  Gemini Pen-Wipes

First Coat  
Gemini Lacquer Sanding Sealer
Second Coat  
Gemini Clear Lacquer
Third Coat 
Gemini Clear Lacquer

G. SMOOTH WOOD CLEAR VARNISH (HIGH PERFORMANCE)

Stain:  Gemini Pen-Wipes

First Coat  
Gemini Conversion Varnish
Second Coat  
Gemini Conversion Varnish

H. GALVANIZED METAL AND ALUMINUM

Flat:

Pretreatment  Galva-Grip (Wash)
First Coat 
1736 Excel Primer (100% Acrylic)
Second Coat  
1776 Super Flat (Vinyl Acrylic)

Satin:

Pretreatment  Galva-Grip (Wash)
First Coat  
1736 Excel Primer (100% Acrylic)
Second Coat  
1770 Super Satin (100% Acrylic)

Semi-Gloss:

Pretreatment  Galva-Grip (Wash)
First Coat 
1736 Excel Primer (100% Acrylic)
Second Coat  
1745 Super Semi-Gloss (100% Acrylic)

Gloss:

Pretreatment  Galva-Grip (Wash)
First Coat  
1736 Excel Primer (100% Acrylic)
Second Coat  
1751 Excel Gloss (100% Acrylic)  or
Tech-Gard Gloss Enamel (Alkyd)

I. FERROUS METAL (IRON & STEEL)

Flat:

First Coat  
E-155 Red Oxide Primer
Second Coat 
1776 Super Flat (Vinyl Acrylic)
Third Coat  
1776 Super Flat ( Vinyl Acrylic)

Satin:

First Coat  E-155 Red Oxide Primer
Second Coat  1770 Super Satin (100% Acrylic)
Third Coat  1770 Super Satin (100% Acrylic)
.
Semi-Gloss:

First Coat  E-155 Red Oxide Primer
Second Coat  1745 Semi-Gloss (100% Acrylic)
Third Coat  1745 Semi-Gloss (100% Acrylic)

Gloss:

First Coat  E-155 Red Oxide Primer
Second Coat  1751 Excel Gloss Enamel
Third Coat  1751 Excel Gloss Enamel

End Of Painting Section