RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT FLOOR UNDERLAYMENT FOR CAPPING CAST IN PLACE CONCRETE, PRECAST OR HOLLOWCORE PLANK

PART 1 GENERAL

1.01    SUMMARY

- Description of Work: Work of this section includes underlayment for interior finish flooring and is not limited to the following:

  - Maxxon Level-Right Floor Underlayment covering normal project conditions and applications.

  - Division 3 Section-Concrete: “Cast Underlayment”

  - Division 9 Section-Finishes: “Acoustic Treatment”

  - REFERENCES

- Underwriters Laboratory 		Fire Resistance Volume 1

www.ul.com

- GREENGUARD Certified	GREENGUARD and GREENGUARD Gold Certified

www.greenguard.org

- ASTM E336 and E1007		Field Sound Transmission Class (F-STC), Field

Impact Insulation Class (F-IIC)

- ASTM E90 and E492		Sound Transmission Class (STC), Impact Insulation

Class (IIC)

- ASTM C109M			Standard Test Method for Compressive Strength of 					Hydraulic Cement Mortars

- ASTM F2170				Standard Test Method for Determining Relative						Humidity in Concrete Floor Slab

- ASTM F2873				Standard Practice for the Installation of Self-Leveling 					Underlayment and Preparation of Surface to Receive 					Resilient Floor Goods

- ASTM F2678				Standard Practice for Preparing Panel Underlayments,

Thick Poured Lightweight Cellular Concrete Underlayments, and Concrete Subfloors with Underlayment Patching Compounds to Receive Resilient Flooring

- TCNA F 180				Tile Council of North America Installation Handbook

www.tileusa.com

- NWFA					National Wood Flooring Association Instructions

www.nwfa.org

- Finished Floor Goods Procedures	Maxxon Procedures for Attaching Finished Floor						Goods to Maxxon Underlayments

www.maxxon.com

1.03    SUBMITTALS

- Product Data: Submit sale sheets Level-Right Sales Sheet, Acousti-Mat Ultimate Sound Control Systems, Acousti-Mat Perimeter Isolation Strips Spec Sheet, Procedures for Attaching Finished Floor Goods to Maxxon Underlayments, and Maxxon’s Building Conditions Guide with project materials clearly identified for each required product or system.

- UL Directory Fire Resistance Volume 1 – See www.maxxon.com for the current list of applicable UL or ULC fire designs.

- Acoustical Data: Submit sound tests according to IBC code criteria ASTM E492 (IIC) and ASTM E90 (STC) or ASTM E1007 (F-IIC) and E336 (F-IIC).

- Code Approvals: See www.maxxon.com for the current list of code approvals.

1.04     SYSTEM REQUIREMENTS

- Performance Requirements:

  - Level-Right Floor Underlayment (An Eco-Friendly building product)

    - Compressive strength up to 5,500 psi (37.9 MPa)

    - Density 125 pounds per cubic foot (2,002 kg/m3)

************This product may contribute to USGBC LEED Credits (MR 3; EQ 2, 4)***********

Potential USGBC LEED Credit Contribution:

a. MR Credit 3: Building Product Disclosure and Optimization - Sourcing Raw Material

b. EQ Credit 2: Low Emitting Materials.

c. EQ Credit 4: Indoor Air Quality Assessment.

Contact Maxxon Corporation for specific details.

******************************************************************************************************

*****Note: The following is for 2009 IBC Acoustical Requirements Section 1207*****

  - Sound Control – 2009 International Building Code: Section 1207.2 & .3

    - Minimum Sound Transmission Class, 50 STC (45 if field tested) – Section 1207.2

      - ASTM E90 and E336

    - Minimum Impact Insulation Class, 50 IIC (45 if field tested) – Section 1207.3

      - ASTM E492 and E1007

1.05    QUALITY ASSURANCE

- Performance Standards:

  - All materials, unless otherwise indicated, shall be manufactured by Maxxon Corporation and shall be installed in accordance with its current printed directions and by a Maxxon Corporation Authorized Applicator.

  - Underlayment mix shall be tested for a slump using a 2" (i.d.) x 4" (50 mm x 101 mm) cylinder resulting in a patty size of 9 ½ inches (241 mm) plus or minus 1 inch (25 mm) diameter.

  - Compressive strength tested in accordance with ASTM C109M.

1.06    DELIVERY, STORAGE AND HANDLING

- All materials shall be delivered in their original unopened packages and protected from damage and exposure from the elements. Damaged or deteriorated materials shall be removed from the premises.

1.07    PROJECT CONDITIONS

- Before, during and after installation of product, building interior shall be enclosed, with adequate ventilation and heat maintained at a temperature above 50 °F (10 °C) to allow for drying of product.

PART 2 GENERAL

2.01    PRODUCTS AND MANUFACTURERS

A.  Manufacturer: Maxxon Corporation, Hamel, MN; A WEBNC Certified Business Enterprise. Telephone: (800) 356-7887.

2.02    MATERIALS

- Proprietary products/systems: Poured flooring underlayment and topping products, including the following:

  - Level-Right Floor Underlayment

*****Note: The following is for 2009 IBC Acoustical Requirements Section 1207*****

- Proprietary products/systems: Optional Sound Control that does not negate the fire rating and is specified in UL design. Acoustical performance is dependent on system design and construction.

  - Acousti-Mat® 1/8 Sound Mat

  - Acousti-Mat® 1/4 Sound Mat

  - Acousti-Mat® 14 Premium Sound Mat

  - Acousti-Mat® 3/8 Sound Mat

  - Acousti-Mat® 3/8 Premium Sound Mat

  - Acousti-Mat® 3/4 Sound Mat

  - Acousti-Mat® 3/4 Premium Sound Mat

************These products may contribute to USGBC LEED Credits (EQ 2, 4, 9)************

Potential USGBC LEED Credit Contribution:

a. EQ Credit 2: Low Emitting Materials.

b. EQ Credit 4: Indoor Air Quality Assessment.

c. EQ Credit 9: Acoustic Performance.

Contact Maxxon Corporation for specific details.

******************************************************************************************************

- Maxxon Acousti-Mat Perimeter Isolation Strips as manufactured by Maxxon Corporation, Hamel, MN

- Maxxon Acousti-Mat Tape as manufactured by Maxxon Corporation, Hamel, MN

- Maxxon Floor Primer:

  - Material Standard: Comply with specifications outlined in manufacturer's Design and Installation.

- Mix Water:

  - Material Standard: Potable, free from impurities and from a domestic source.

- Sand Aggregate:

  - Sand shall meet Maxxon Sand Specification 101.

- Maxxon Overspray Primer Sealer:

  - Seal all areas that receive glue down floor goods with Maxxon Overspray according to manufacturer's specifications.

- Maxxon Acrylic Sealer (Alternate to Overspray):

  - Seal all areas that receive glue down floor goods with Maxxon Acrylic according to manufacturer’s specifications.

- Maxxon Reinforcement:

  - Install approved reinforcement as per manufacturer recommendations.

PART 3 EXECUTION

3.01    EXAMINATION

- Site Verification of Conditions:

  - Installation shall not begin until the building is enclosed, including roof, windows, doors, and any other apertures.

  - Concrete substrate shall be structurally sound, properly fastened and dry. Contractor shall clean subfloor to remove mud, oil, grease and construction debris before arrival of the authorized applicator.

  - Maxxon Level-Right is not a vapor barrier. The general contractor, architect, specifier, or building owner shall test below grade, on grade, or elevated slabs for MVER (ASTM F1869-16) or RH (ASTM F2170). If the MVER or RH of the concrete substrate exceeds the floor covering manufacturer’s respective requirements for the finished floor system, the concrete should be treated with a moisture vapor barrier, such as Aquafin® Vaportight Coat® SG2, SG3 or SG4, before installing Level-Right.

3.02    REQUIREMENTS

- Leak Prevention:

  - Fill cracks and voids in subfloor where leakage of slurry could occur.

- Priming subfloor:

  - Prime substrate according to manufacturer's recommendations.

- Application:

  - Install in accordance with reference standards and manufacturer's instructions.

3.03    GENERAL INSTALLATION REQUIREMENTS

- Mixing Proportions:

  - General Requirements: Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

- Application:

  - (Optional) Acousti-Mat Installations:  Install Acousti-Mat following manufacturer’s recommendations and specifications including installation of Perimeter Isolation Strips at the perimeter of all areas receiving Acousti-Mat (including doorframes) and around any protrusions through the installation.  Adhere the foam perimeter isolation strip to the wall with Acousti-Mat Tape.

  - Pour floor topping to recommended thickness. Immediately spread and screed product to a smooth surface.  Expansion joints in all types of work shall be brought through the underlayment.

    - Recommended Minimum Level-Right Underlayment Depth 0 – 3” (0 – 76 mm).

    - If applying over an Acousti-Mat Sound Control Mat, consult Maxxon Corporation for depth requirements.

- Drying:

  - The general contractor must provide and maintain correct environmental conditions to keep the building clean and dry, and protect against infestation of moisture from a variety of potential sources.  The general contractor must supply mechanical ventilation and heat if necessary to remove moisture from the area until the Level-Right is dry.

  - Protection from Heavy Loads:  During construction, place temporary wood planking over Level-Right wherever it will be subject to heavy wheeled or concentrated loads.

  - PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

- Sealing:

  - Seal all areas that receive glue down floor goods with Maxxon Overspray or Maxxon Acrylic according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

  - Maxxon UWR can be used over Maxxon underlayments in low traffic areas such as utility rooms, storage rooms and closets, as a protective surface.

- Moisture Testing:

  - Follow the respective floor goods manufacturers’ recommendations for relative humidity requirements.  When manufacturer does not have a relative humidity requirement, refer to Maxxon’s Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure.

- Finished Floor Goods:

  - There are many reference standards for the installation procedures and recommendations for finished flooring applications over gypsum underlayments.  These include instructions of the manufacturers of the finished flooring, adhesives and thin-set as well as national agency reference standards.  The national standards are listed below:

| Flooring Type | Reference Standard |
| --- | --- |
| Resilient | ASTM F2873 |
| Ceramic Tile | TCNA F180 |
| Wood | NWFA Instructions |

See Maxxon Corporation's Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

END OF SECTION